FICTITIOUS DEMONSTRATION SAMPLE

Tab 4: Manufacturer and quality records

FICTIONAL DEMONSTRATION SAMPLE. The certificates, signatures, test values, report numbers, and entities in this tab are invented.

# 4A. Calder manufacturer Certificate of Conformance

Calder Fluid Systems Corp, CAGE 0DEM7, certifies that lot CFS-L2606-118, part CFS-2205-7, was manufactured and inspected to drawing CFS-2205 revision C. The lot uses 17-4 PH stainless steel from heat 6L-4471 and passed the lot tests summarized below. This manufacturer record supports NSN 4820-01-DEM-0755 and quantity 150 EA offered under SPE7L0-26-R-DEM4.

Certificate: CFS-COC-2606-118 Date: 2026-06-11 Authorized by: /s/ Amina Cole, Quality Manager (FICTIONAL SAMPLE)

# 4B. Certified material test report

| Field | Result |
| --- | --- |
| Mill | Tri-State Alloy Mill, CAGE 7DEM9 |
| Report | TSA-6L-4471, dated 2026-03-04 |
| Material | 17-4 PH stainless bar, condition H1025, AMS 5643 |
| Heat | 6L-4471 |
| Chemistry, weight percent | C 0.04; Cr 15.8; Ni 4.3; Cu 3.4; Mn 0.7; Si 0.6; S 0.008; P 0.020 |
| Mechanical results | Tensile 155 ksi; yield 145 ksi; elongation 14 percent; hardness 34 HRC |
| Disposition | Accepted for Calder lot CFS-L2606-118 |

Certified by: /s/ Leah Hammond, Laboratory Manager (FICTIONAL SAMPLE) Date: 2026-03-04

# 4C. Lot test reports

| Test | Record | Population or sample | Result |
| --- | --- | --- | --- |
| Proof pressure | CFS-PPT-2606-118, 2026-06-10 | 260 of 260 units at 4,500 psi for 3 minutes | 260 passed; no external leakage |
| Seat leakage | CFS-SLT-2606-118, 2026-06-10 | 260 of 260 units at rated pressure | 260 passed; no reject recorded |
| Dimensional check | CFS-DIM-2606-118, 2026-06-10 | 13-piece sample against drawing revision C | 13 passed; zero recorded defects |

Approved by: /s/ Amina Cole, Quality Manager (FICTIONAL SAMPLE) Date: 2026-06-11

# 4D. Meridian incoming inspection

Receiving record GRN-8DEM2-3390 references Ardent packing slip AFD-PS-24817. Inspection record IR-8DEM2-3390 confirms part CFS-2205-7, drawing revision C marking, lot CFS-L2606-118, clean capped ports, and 260 units received. Meridian accepted the lot on 2026-06-23.

Inspector: /s/ Theo Marsh, Purchasing and Receiving (FICTIONAL SAMPLE)

# 4E. Higher-level quality evidence

| Organization | ISO 9001:2015 evidence | Status used for this quote |
| --- | --- | --- |
| Meridian Precision Components, Inc. | MPC-ISO-2025-114, expires 2028-04-30 | Current; status checked 2026-06-30 |
| Calder Fluid Systems Corp | CFS-QMS-2024-088, expires 2027-11-30 | Current; status checked 2026-06-30 |
| Juniper Vale Packaging LLC | JVP-QMS-2025-041, expires 2028-02-28 | Current; status checked 2026-06-30 |

The offeror rechecks all certificate dates before a live submission. This fictional tab records the completed check for the sample package.