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FICTITIOUS DEMONSTRATION SAMPLE
Tab 4: Manufacturer and quality records
	FICTIONAL DEMONSTRATION SAMPLE. The certificates, signatures, test values, report numbers, and entities in this tab are invented.


4A. Calder manufacturer Certificate of Conformance
Calder Fluid Systems Corp, CAGE 0DEM7, certifies that lot CFS-L2606-118, part CFS-2205-7, was manufactured and inspected to drawing CFS-2205 revision C. The lot uses 17-4 PH stainless steel from heat 6L-4471 and passed the lot tests summarized below. This manufacturer record supports NSN 4820-01-DEM-0755 and quantity 150 EA offered under SPE7L0-26-R-DEM4.
Certificate: CFS-COC-2606-118 Date: 2026-06-11 Authorized by: /s/ Amina Cole, Quality Manager (FICTIONAL SAMPLE)
4B. Certified material test report
	Field
	Result

	Mill
	Tri-State Alloy Mill, CAGE 7DEM9

	Report
	TSA-6L-4471, dated 2026-03-04

	Material
	17-4 PH stainless bar, condition H1025, AMS 5643

	Heat
	6L-4471

	Chemistry, weight percent
	C 0.04; Cr 15.8; Ni 4.3; Cu 3.4; Mn 0.7; Si 0.6; S 0.008; P 0.020

	Mechanical results
	Tensile 155 ksi; yield 145 ksi; elongation 14 percent; hardness 34 HRC

	Disposition
	Accepted for Calder lot CFS-L2606-118



Certified by: /s/ Leah Hammond, Laboratory Manager (FICTIONAL SAMPLE) Date: 2026-03-04
4C. Lot test reports
	Test
	Record
	Population or sample
	Result

	Proof pressure
	CFS-PPT-2606-118, 2026-06-10
	260 of 260 units at 4,500 psi for 3 minutes
	260 passed; no external leakage

	Seat leakage
	CFS-SLT-2606-118, 2026-06-10
	260 of 260 units at rated pressure
	260 passed; no reject recorded

	Dimensional check
	CFS-DIM-2606-118, 2026-06-10
	13-piece sample against drawing revision C
	13 passed; zero recorded defects



Approved by: /s/ Amina Cole, Quality Manager (FICTIONAL SAMPLE) Date: 2026-06-11
4D. Meridian incoming inspection
Receiving record GRN-8DEM2-3390 references Ardent packing slip AFD-PS-24817. Inspection record IR-8DEM2-3390 confirms part CFS-2205-7, drawing revision C marking, lot CFS-L2606-118, clean capped ports, and 260 units received. Meridian accepted the lot on 2026-06-23.
Inspector: /s/ Theo Marsh, Purchasing and Receiving (FICTIONAL SAMPLE)
4E. Higher-level quality evidence
	Organization
	ISO 9001:2015 evidence
	Status used for this quote

	Meridian Precision Components, Inc.
	MPC-ISO-2025-114, expires 2028-04-30
	Current; status checked 2026-06-30

	Calder Fluid Systems Corp
	CFS-QMS-2024-088, expires 2027-11-30
	Current; status checked 2026-06-30

	Juniper Vale Packaging LLC
	JVP-QMS-2025-041, expires 2028-02-28
	Current; status checked 2026-06-30



The offeror rechecks all certificate dates before a live submission. This fictional tab records the completed check for the sample package.
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